TECHNICAL DATA SHEET

Butyl Rubber VS 6800 ( Hexpol Compounding UK) 4 x 1100 x 10000mm Chemical Resistant

Description	:         	Butyl Rubber VS 6800 ( Hexpol Compounding UK) 4 x 1100 x 10000mm Chemical Resistant

is a high quality bromobutyl rubber specifically compounded for use as a plant

Plant Lining material .

The compound is resistant to a very wide range of chemicals including acids and alkalis at elevated temperatures.

For specific applications refer to HEXPOL Compounding or see the chemical resistance data chart.

Temperature	:	Depending upon application -20 to 100oC.

Range

Hardness	:	55 Shore A

S.G.		:	1.22

Bonding	:	Two part - Chemosil 211 / Chemosil X6025 / Butyl tack solution.

System		One part - Cilbond 89E / Butyl tack solution.

Cure Time	:	Autoclave cure for 1.5 hours at 150oC (55 psi, 3.6 bar) or site cure,

preferably under water for 16 hours at 95/100oC

Issue:	4

Date:	07.06.2011.

HEXPOL Compounding (UK) Ltd

Fifth Avenue

Tameside Park

Dukinfield

Cheshire SK16 4PP

England

HEXPOL Compounding (UK) Ltd										       Tel: +44 (0)161 343 4433

Incorporating Chase Elastomer (UK) Ltd									      Fax: +44 (0)161 343 4422

Registered Office; Unit 3, Fifth Avenue, Tameside Park, Dukinfield Cheshire, SK16 4PP					  info@excel-polymers.co.uk

Company No.: 05172769										     www.excel-polymers.com